| Ferric Chloride |  |
| --- | --- |
| DESCRIPTION |  |
| Anhydrous solid |  |
| Physical Properties |  |
| Molecular Weight | 162,2 |
| Specific Density | 2,9 |
| pH (Sol. 1%) |  |
| Deteriorates Above | 300 ºC |
| Chemical Composition |  |
| Chemical Formula | FeCl3 |
| FeCl3 | 96% max |
| FeCl2 | 2,00% |
| H2O (%) |  |
| Water Insolubles (%) | 1,5% max |
| As (method limit = 2ppm) | 0,002% max |
| Hevy Metals (Pb) (method limit = 2ppm) | 0,004% max |
| Packaging |  |
| Others | Up on request |
| Validity |  |
| One Year if properly storage in a dry warehouse |  |
| The Registry of Toxic Effects of Chemical Substances |  |
| CAS No: 7705-08-0 |  |