| Magnesium Hydroxide |  |
| --- | --- |
| DESCRIPTION |  |
| Medicinally it, in the form of a mixture (milk of magnesia), is also used as an antacid and as a osmotic laxative. |  |
| Physical Properties |  |
| Molecular Weight | 58,31 |
| Specific Gravity | 2,36 |
| pH (Sol. 1%) | 9,5 - 10,5 |
| Deteriorates Above (ºC) | 350 |
| Chemical Composition |  |
| Chemical Formula | Mg(OH)2 |
| Mg(OH)2 (dry) | 96,00% min. |
| CaO | 1,5% max. |
| Loss on ignition | 30,5% max. |
| Solubles Salts | 0,5% max. |
| Packaging |  |
| 50 kgs bag | Usual |
| Others | Up on request |
| Validity |  |
| One Year if properly storage in a dry warehouse |  |
| The Registry of Toxic Effects of Chemical Substances |  |
| CAS No: 1309-42-8 |  |